Comparison of

No.47 Shipbuilding and Repair Quality Standard

(1996) 
(Rev. 1, 1999) 
(Rev.2, Dec. 2004)

with

Japan Shipbuilding Quality Standard (JSQS, 1004, Appendix 0144

and

Production Standard of the German Shipbuilding Industry (FS, 2003)

PART A - SHIPBUILDING AND REPAIR QUALITY STANDARDS FOR NEW CONSTRUCTION

1. Scope

2. General requirements for new construction

3. Qualification of personnel and procedures

3.1 Qualification of welders
3.2 Qualification of welding procedures 
3.3 Qualification of NDE operators

4. Materials

4.1 Materials for structural members 
4.2 Under thickness tolerances 
4.3 Surface conditions

5. Cutting

5.1 Gas cutting 
5.2 Plasma arc cutting 
5.3 Laser beam cutting

6. Fabrication and fairness

6.1 Flangedlongitudinals and flangedbrackets 
6.2 Built-up sections 
6.3 Corrugated bulkheads 
6.4 Pillars, brackets and stiffeners 
6.5 Maximum heating temperature on surface for line heating 
6.6 Block assembly
6.7 Special sub-assembly 
6.8 Shape 
6.9 Fairness of plating between frames 
6.10 Fairness of plating with frames 
6.11 Preheating for welding hull steels at low temperature

7. Alignment

8. Welding

8.1 Typical butt weld plate edge preparation (manual welding) 
8.2 Typical fillet weld plate edge preparation (manual welding) 
8.3 Typical butt and fillet weld profile (manual welding)
8.4 Lap, plug and slot welding
8.5 Distance between welds 
8.6 Automatic welding

9. Repair

9.1 Typical misalignment repair 
9.2 Typical butt weld plate edge preparation repair (manual welding) 
9.3 Typical fillet weld plate edge preparation repair (manual welding)
9.4 Typical fillet and butt weld profile repair (manual welding) 
9.5 Distance between welds repair 
9.6 Erroneous hole repair 
9.7 Repair by insert plate 
9.8 Weld surface repair

REFERENCES

1. IACS “Bulk Carriers - Guidelines for Surveys, Assessment and Repair of Hull Structure”

2. TSCF “Guidelines for the inspection and maintenance of double hull tanker structures”

3. TSCF “Guidance manual for the inspection and condition assessment of tanker structures”

4. IACS UR W7 “Hull and machinery steel forgings”

5. IACS UR W8 “Hull and machinery steel castings”

6. IACS UR W11 “Normal and higher strength hull structural steel”

7. IACS UR W13 “Allowable under thickness tolerances of steel plates and wide flats”

8. IACS UR W14 “Steel plates and wide flats with improved through thickness properties”

9. IACS UR W17 “Approval of consumables for welding normal and higher strength hull structural steels”

10. IACS UR Z10.1 “Hull surveys of oil tankers” and Z10.2 “Hull surveys of bulk carriers” Annex I

11. IACS Recommendation No. 12 “Guidelines for surface finish of hot rolled plates and wide flats “

13. IACS Recommendation No. 20 “ Guide for inspection of ship hull welds”

1. 	Scope

1.1	This standard provides guidance on shipbuilding quality standards for the hull structure during new construction and the repair standard where the quality standard is not met.

Whereas the standard generally applies to

-	conventional ship types,

-	parts of hull covered by the rules of the Classification Society,

-	hull structures constructed from normal and higher strength hull structural steel, the applicability of the standard is in each case to be agreed upon by the Classification Society.

The standard does generally not apply to the new construction of

-	special types of ships as e.g. gas tankers -structures fabricated from stainless steel or other, special types or grades of steel

1.2	The standard covers typical construction methods and gives guidance on quality standards for the most important aspects of such construction. Unless explicitly stated elsewhere in the standard, the level of workmanship reflected herein will in principle be acceptable for primary and secondary structure of conventional designs. A more stringent standard may however be required for critical and highly stressed areas of the hull, and this is to be agreed with the Classification Society in each case. In assessing the criticality of hull structure and structural components, reference is made to ref. 1, 2 and 3

1.3	Details relevant to structures or fabrication procedures not covered by this standard are to be approved by the Classification Society on the basis of procedure qualifications and/or recognized national standards.

1.4	It is intended that these standards provide guidance where established shipbuilding or national standards approved by the Classification Society do not exist.

1.5	For use of this standard, fabrication fit-ups, deflections and similar quality attributes are intended to be uniformly distributed about the nominal values. The shipyard is to take corrective action to improve work processes that produce measurements where a skewed distribution is evident. Relying upon remedial steps that truncate a skewed distribution of the quality attribute is unacceptable.

2.	General requirements for new construction

2.1	In general, the work is to be carried out in accordance with the Classification Society rules and under the supervision of the Surveyor to the Classification Society

2.2	Provisions are to be made for proper accessibility, staging, lighting and ventilation. Welding operations are to be carried out under shelter from rain, snow and wind.

2.3	Welding of hull structures is to be carried out by qualified welders, according to approved and qualified welding procedures and with welding consumables approved by the Classification Society, see Section 3. Welding operations are to be carried out under proper supervision by the shipbuilder.

[no equivalent in FS or JSQS]

3. 	Qualification of personnel and procedures

3.1	Qualification of welders

3.1.1	Welders are to be qualified in accordance with the procedures of the Classification Society or to a recognized national or international standard, e.g. EN 287, ISO 9606, ASME Section IX, ANSI/AWS D1.1. Recognition of other standards is subject to submission to the Classification Society for evaluation. Subcontractors are to keep records of welders qualification and, when required, furnish valid approval test certificates.

3.1.2	Welding operators using fully mechanized or fully automatic processes need generally not pass approval testing provided that the production welds made by the operators are of the required quality. However, operators are to receive adequate training in setting or programming and operating the equipment Records of training and production test results shall be maintained on individual operator’s files and records, and be made available to the Classification Society for inspection when requested.

[no equivalent in FS or JSQS]

3.2 Qualification of welding procedures

Welding procedures are to be qualified in accordance with the procedures of the Classification Society or a recognized national or international standard, e.g. EN288, ISO 9956, ASME Section IX, ANSI/AWS D1.1. Recognition of other standards is subject to submission to the Classification Society for evaluation. The welding procedure should be supported by a welding procedure qualification record. The specification is to include the welding process, types of electrodes, weld shape, edge preparation, welding techniques and positions.

[no equivalent in FS or JSQS]

3.3	Qualification of NDE operators

3.3.1	Personnel performing non-destructive examination for the purpose of assessing quality of welds in connection with new construction covered by this standard, are to be qualified in accordance with Classification Society rules or to a recognized international or national qualification scheme. Records of operators and their current certificates are to be kept and made available to the Surveyor for inspection.

[no equivalent in FS or JSQS]

4.	Materials

4.1	Materials for Structural Members

All materials, including weld consumables, to be used for the structural members are to be approved by the Classification Society as per the approved construction drawings and meet the respective IACS Unified Requirements. Additional recommendations are contained in the following paragraphs. All materials used should be manufactured at a works approved by the Classification Society for the type and grade supplied.

[no equivalent in FS or JSQS]

4.2	Surface Conditions

| Detail | JSQS (Tolerance limits) | Rec. 47 (Limit) | VSM (Limit) |
| --- | --- | --- | --- |
| 4.2.2 Unrepaired Conditions | Repair unnecessary: < 20% area ratio and < 0.3 mm depth (Ref. I.A.1/2, pg. 2) | Minor imperfections, in accordance with the limits described in Table 1, are permissible and may be left unrepaired. Area ratio (%); 15～20%; 5～15% ; 0～5%; t < 20mm ; 0.2mm ; 0.4mm ; 0.5mm; 20mm ≤ t < 50mm ; 0.2mm; 0.6mm; 0.7mm ; 50mm ≤ t ; 0.2mm; 0.7mm; 0.9mm ; | Limit acc. to DIN EN 10 163 und DIN EN 10 029, class B (Ref. 1.1., pg. 5) |
| 4.2.3 Repairs of Defects |  | Defects are to be repaired by grinding or welding irrespective of their size and number. Repair by grinding may be carried out over the entire surface up to a depth equal to –0.3mm. |  |
| 4.2.4 Repairs by Grinding | d > 0.07 t, max 3 mm (Ref. I.A.1/2, pg. 2) | The nominal thickness is not to be reduced by more than 7% or 3mm, whichever is the lesser. Each single ground area is not to exceed 0.25m2 . The defects are to be completely removed by grinding. Complete elimination of the defects is to be verified by a magnetic particle or dye penetrant test procedure. The ground areas must have smooth transitions to the surrounding surface. | max. 0,25 m² per local area max. 2 % of the total surface (Ref. 1.2, pg. 6) |
| 4.2.5 Repairs by welding | 0.07 t < d < 0.2 t, max 3 mm (Ref. I.A.1/2, pg. 2) | Local defects, which cannot be repaired by grinding, may be repaired by chipping and/or grinding followed by welding in accordance with the qualified procedures approved by the Classification Society concerned. Any single welded area is not to exceed 0.125m2. The weld preparation should not reduce the thickness of the product below 80% of the nominal thickness. Welding is to be completed with one layer of weld bead in excess, which is subsequently to be ground smooth, level with the plate surface. The soundness of the repair is to be verified by ultrasonic, magnetic particle or dye penetrant methods. | max. 20 % of nominal thickness max. 0,125 m² per local area max. 2 % of the total surface (Ref. 1.2, pg. 6) |
| 4.2.6.1 Lamination | In case where the range of lamination is limited, it can be chipped out and build-up by welding (a). In case where the range of lamination is limited also, but is near the plate surface, it is preferable to make the build-up welding as shown in (b). It is recommended to exchange locally the plate in case where the range of lamination is fairly extensive. The standard minimum breadth of the plate to be exchanged: · 1600mm for shell and strength deck under large constraint, · 800mm not under large constraint, · 300mm for other structural members. (Ref. I.C.1/2, pg. 2) | Severe lamination is to be repaired by local insert plates. The minimum breadth or length of the plate to be replaced is to be: · 1600mm for shell and strength deck plating in way of cruciform or T-joints, · 800mm for shell, strength deck plating and other primary members, · 300mm for other structural members. Local limited lamination may be repaired by chipping and/or grinding followed by welding in accordance with sketch (a). In case where the local limited lamination is near the plate surface, the repair may be carried out as shown in sketch (b). | Length and width of insert plate: L and B > 300 mm or 10 t (Ref. 1.1.5, pg. 7) |
| Detail | JSQS (Tolerance limits) | Rec. 47 (Limit) | VSM (Limit) |
| 4.2.6.2 Weld Spatters | ? | Loose weld spatters are to be removed completely by grinding to clean metal (see Table 9.13) on: · shell plating · deck plating on exposed decks · in tanks for chemical cargoes · in tanks for fresh water and for drinking water · in tanks for lubricating oil, hydraulic oil, including service tanks | Loose weld splatter will be removed on: · Areas insulated from outside · decks underneath deck covering · Cargo holds · Exposed decks incl. deck outfits, shell topside and superstructures · Underwater areas of shell, pools · Visible areas within engine rooms, store rooms, service and technical rooms, shops, kitchens, living rooms and service routes (above 2m height) · behind ceilings, underneath insulation and cladding · within service routes · cargo holds · voids, cofferdams · BW tanks · Crude oil tanks · Slop tanks, grey water and dirt water tanks, boiler water tanks and distillate tanks · Tanks for fresh water and drinking water (Ref. 3.3.1, Table 2, pg. 11) |

5. Cutting

| Detail | JSQS (Tolerance limits) | Rec. 47 (Limit) | VSM (Limit) |
| --- | --- | --- | --- |
| 5.1 Gas Cutting Roughness | Mechanised gas cutting: R=200/200 µm Manual gas cutting / free edges: R=300/1000 µm Manual gas cutting / welding edges: R=800/1500 µm (Ref. III.A.1/2, pg. 4) | Mechanised gas cutting: R=150 µm Manual gas cutting / free edges: R=300/500 µm Manual gas cutting / welding edges: R=800/1500 µm | ? |
| Individual non-sharp notches caused by torch failure Free edges of members: Sheer strake etc Longitudinal and transverses Others | No notch < 1.0mm < 3.0mm (Ref. III.B.1/2, pg. 4) | No notch < 1.0mm < 3.0mm | ? |
| Weld edges: Butt weld, Shell plate and strength deck in 0.6L amidship Butt weld, Others Fillet weld | < 2.0mm < 3.0mm < 3.0mm (Ref. III.B.1/2, pg. 4) | < 2.0mm < 3.0mm < 3.0mm |  |

6.	Fabrication and fairness

6.1 Flanged longitudinals and flanged brackets (see Table 6.1)

6.2 Built-up sections (see Table 6.2)

6.3 Corrugated bulkheads (see Table 6.3)

6.4 Pillars, brackets and stiffeners (see Table 6.4)

6.5 Maximum heating temperature on surface for line heating (see Table 6.5)

6.6 Block assembly (see Table 6.6)

6.7 Special sub-assembly (see Table 6.7)

6.8 Shape (see Table 6.8 and 6.9)

6.9 Fairness of plating between frames (see Table 6.10)

6.10 Fairness of plating with frames (see Table 6.11)

6.11 Preheating for welding hull steels at low temperature (See Table 6.12)

7. Alignment

The quality standards for alignment of hull structural components during new construction are shown in Tables 7.1, 7.2 and 7.3. The Classification Society may require a closer construction tolerance in areas requiring special attention, as follows:

·	Regions exposed to high stress concentrations

·	Fatigue prone areas

·	Detail design block erection joints

·	Higher tensile steel regions

8.		Welding Details

8.1 Typical butt weld plate edge preparation (manual welding) - see Table 8.1 and 8.2

8.2 Typical fillet weld plate edge preparation (manual welding) - see Table 8.3 and 8.4

8.3 Typical butt and fillet weld profile (manual welding) - see Table 8.5

8.4 Lap, plug and slot welding - see Table 8.6

8.5 Distance between welds - see Table 8.7

8.6 Automatic welding - see Table 8.8

9.		Repair

9.1 Typical misalignment repair - see Tables 9.1 to 9.3

9.2 Typical butt weld plate edge preparation repair (manual welding) - see Table 9.4 and 9.5

9.3 Typical fillet weld plate edge preparation repair (manual welding) - see Tables 9.6 to 9.8

9.4 Typical fillet and butt weld profile repair (manual welding) - see Table 9.9

9.5 Distance between welds repair - see Table 9.10

9.6 Erroneous hole repair - see Table 9.11

9.7 Repair by insert plate - see Table 9.12

9.8 Weld surface repair - see Table 9.13

TABLE 6.1 – Flanged Longitudinals and Flanged Brackets

| Detail | JSQS (Tolerance limits) | Rec. 47 (Limit) | VSM (Limit) |
| --- | --- | --- | --- |
| Breadth of flange compared to correct size | 5 mm (Ref. IV.A.1, pg. 6) | 5 mm | - 5 mm per 100 mm, max. 15 mm (Ref. 4.1.1, pg. 12) |
| Angle between flange and web compared to template | 4,5 mm per 100 mm of a (Ref. IV.A.1, pg. 6) | 5 mm per 100 mm of a | 5 mm per 100 mm of a (Ref. 4.1.1, pg. 12) |
| Straightness in plane of flange and web | 25 mm per 10 m (Ref. IV.A.4 + 5, pg. 6) | 25 mm per 10 m | ? |

TABLE 6.2 – Built Up Sections

| Detail | JSQS (Tolerance limits) | Rec. 47 (Limit) | VSM (Limit) |
| --- | --- | --- | --- |
| Frames and longitudinal | 3 mm (absolute?) (Ref. IV.D.2, pg. 7) | 3 mm per 100 mm of a | 5 mm per 100 mm of a (Ref. 4.1.1, pg. 12) |
| Distortion of face plate | d ≤ 5 + a/100 mm (Ref. IX.C.6, pg. 23) | d ≤ 5 + a/100 mm | 5 mm per 100 mm of a (Ref. 4.1.2, pg. 12) |
| Distortion of girder and transverse at upper edge and flange | 8 mm per length of span (Ref. IX.C.1, pg. 23) | 8 mm per span between primary members |  |

TABLE 6.3 – Corrugated Bulkheads

| Detail | JSQS (Tolerance limits) | Rec. 47 (Limit) | VSM (Limit) |
| --- | --- | --- | --- |
| Mechanical bending | ? | R ≥ 3 t mm Material to be suitable for cold flanging (forming) and welding in way of radius | ? |
| Depth of corrugation | 6 mm (Ref. IV.E.1, pg. 8) | 6 mm | 0,5 t (Ref. 4.1.3, pg. 12) |
| Breadth of corrugation web |  | 6 mm | can be deduced from the breath of corrugation; if required it should be the double value of for the breath of corrugation tolerance |
| Breadth of corrugation | 6 mm (Ref. IV.E.1, pg. 8) | 6 mm | not limited or 0,5 t (Ref. 4.1.3, pg. 12) |
| Pitch and depth of swedged corrugated bulkhead compared with correct value | h : 5 mm In case where it does not connect with others P : 9 mm In case where it connects with others P : 3 mm (Ref. IV.E.2, pg. 8) | h : 5 mm Where it is not aligned with other bulkheads P : 9 mm Where it is aligned with other bulkheads P : 3mm | ? |

TABLE 6.4 – Pillars, Brackets and Stiffeners

| Detail | JSQS (Tolerance limits) | Rec. 47 (Limit) | VSM (Limit) |
| --- | --- | --- | --- |
| Pillar (between decks) | 6 mm (Ref. IX.C.3, pg. 23) | 6 mm | ? |
| Cylindrical structure diameter (pillars, masts, posts, etc.) | D/150 mm max. 7,5 mm (Ref. IV.E.3, pg. 8) | D/150 mm max. 7,5 mm | ? |
| Tripping bracket and small stiffener, distortion at the part of free edge | t (Ref. IX.C.3, pg. 23) | max. 8 mm | ? |
| Snipe end of secondary face plates and stiffeners |  | θ°= 30° H = 15 mm: + 5 mm - 5 mm D = 25 mm: + 10 mm - 5 mm F = 15 mm: ± 5 mm |  |

TABLE 6.5  Maximum Heating Temperature on Surface for Line Heating

| Item | JSQS (Tolerance limits) | Rec. 47 (Limit) | VSM (Limit) |
| --- | --- | --- | --- |
| Conventional Process AH32-EH32 & AH36-EH36 | Water cooling just after heating | Under 650°C | Under 650°C | ? |
| TCMP type AH32-EH32 & AH36-EH36 (Ceq.>0.38%) | Air cooling after heating | Under 900°C | Under 900°C | ? |
|  | Water cooling subsequent water cooling after heating | Under 900°C (starting temperature of water cooling to be under 500°C) | Under 900°C (starting temperature of water cooling to be under 500°C) |  |
| TMCP type AH32-DH32 & AH36-DH36 (Ceq. ≤ 0.38%) | Water cooling just after heating or air cooling | Under 1000°C | Under 1000°C | ? |
| TMCP type EH32 & EH36 (Ceq. ≤ 0.38%) | Water cooling just after heating or air cooling | Under 900°C (starting temperature of water cooling to be under 550°C) (Ref. IV.F.1, pg. 9) | Under 900°C (starting temperature of water cooling to be under 550°C) | ? |

TABLE 6.6 – Block Assembly

| Item | JSQS (Tolerance limits) | Rec. 47 (Limit) | VSM (Limit) |
| --- | --- | --- | --- |
| Flat Plate Assembly | (Ref. V.A.1, pg. 10) |  | ? |
| Length and Breadth | ± 6 mm | ± 6 mm |  |
| Distortion | 20mm | ± 20 mm |  |
| Squareness | 8 mm | ± 10 mm |  |
| Deviation of interior members from plate | ± 10 mm | 10 mm |  |
| Curved plate assembly | (Ref. V.A.2, pg. 10) |  | ? |
| Length and Breadth | ± 8 mm | ± 8 mm measured along the girth |  |
| Distortion | 20 mm | ± 20 mm |  |
| Squareness | 15 mm | ± 15 mm |  |
| Deviation of interior members from plate | ± 10 mm | 10 mm |  |
| Flat cubic assembly | (Ref. V.A.3, pg. 10/11) |  | ? |
| Length and Breadth | ± 6 mm | ± 6 mm |  |
| Distortion | 20mm | ± 20 mm |  |
| Squareness | 8 mm | ± 10 mm |  |
| Deviation of interior members from plate | ± 10 mm | 10 mm |  |
| Twist | 20 mm | ± 20 mm |  |
| Deviation between upper and lower plate | 10 mm | ± 10 mm |  |
| Curved cubic assembly | (Ref. V.A.4, pg. 11) |  | ? |
| Length and Breadth | ± 6 mm | ± 8 mm measured along with girth |  |
| Distortion | 20mm | ±20mm |  |
| Squareness | 8 mm | ±15mm |  |
| Deviation of interior members from plate | ± 10 mm | ±10mm |  |
| Twist | 25 mm | ±25mm |  |
| Deviation between upper and lower plate | 15 mm | ±15mm |  |

TABLE 6.7 – Special Sub-Assembly

| Item | JSQS (Tolerance limits) | Rec. 47 (Limit) | VSM (Limit) |
| --- | --- | --- | --- |
| Distance between upper/lower gudgeon | ± 10 mm (Ref. V.A.5(a), pg. 11) | ± 10 mm | ? |
| Distance between aft edge of boss and aft peak bulkhead | ± 10 mm (Ref. V.A.5(b), pg. 12) | ± 10 mm | ? |
| Twist of sub-assembly of stern frame | 10 mm (Ref. V.A.5(c), pg. 12) | 10 mm | ? |
| Deviation of rudder from shaft center line | 15 mm (Ref. V.A.5, pg. 12) | 8 mm | ? |
| Twist of rudder plate | 10 mm (Ref. V.A.5, pg. 12) | 10 mm | ? |
| Flatness of top plate of main engine bed | 10 mm (Ref. V.A.5, pg. 12) | 10 mm | ? |
| Breadth and length of top plate of main engine bed | ± 6 mm (Ref. V.A.5, pg. 12) | 6 mm | ? |

TABLE 6.8 – Shape

| Detail | JSQS (Standard range) | Rec. 47 (Standard) | VSM (Limit) |
| --- | --- | --- | --- |
| Deformation for the whole length | ± 25 mm (Ref. VI.B.1, pg. 13) | ± 50 mm per 100 m against the line of keel sighting | ? |
| Deformation for the distance between two adjacent bulkheads | ± 15 mm (Ref. VI.B.1, pg. 13) | ± 15 mm | ± 25 mm per 100 m length (Ref. 9.2.1, pg. 27) |
| Cocking-up of fore body | ± 30 mm (Ref. VI.B.2, pg. 13) | ± 30 mm | + 50 mm - 25 mm (Ref. 9.2.2, pg. 27) |
| Cocking-up of aft-body | ± 20 mm (Ref. VI.B.2, pg. 13) | ± 20 mm | + 50 mm - 25 mm (Ref. 9.2.2, pg. 27) |
| Rise of floor amidships | ± 15 mm (Ref. VI.B.3, pg. 13) | ± 15 mm | ± 25 mm for 10 m of the half breadth (Ref. 9.2.3, pg. 28) |

TABLE 6.9 – Shape

| Item | JSQS (Standard range) | Rec. 47 (Standard) | VSM (Limit) |
| --- | --- | --- | --- |
| Length between perpendiculars | ± 50 mm per 100m Applied to ships of 100 metre length and above. For the convenience of the measurement the point where the keel is connected to the curve of the stern may be substituted for the fore perpendicular in the measurement of the length. (Ref. VI.A.1, pg. 12) | ± 50 (?) per 100 m Applied to ships of 100 metre length and above. For the convenience of the measurement the point where the keel is connected to the curve of the stern may be substituted for the fore perpendicular in the measurement of the length. | ± 100 mm per 100 m length (Ref. 9.1.1, pg. 27) |
| Length between aft edge of boss and main engine | ± 25 mm (Ref. VI.A.1, pg. 12) | ± 25 mm |  |
| Moulded breadth at midship | ± 15 mm Applied to ships of 15 metre breadth and above. Measured on the upper deck. (Ref. VI.A.2, pg. 12) | ± 15 mm Applied to ships of 15 metre breadth and above. Measured on the upper deck. | ± 15 mm per 10 m breadth, max. 40 mm (Ref. 9.1.2, pg. 27) |
| Moulded depth at midship | ± 10 mm Applied to ships of 10 metre depth and above. (Ref. VI.A.3, pg. 12) | ± 10 mm Applied to ships of 10 metre depth and above. | - 10 mm per 10 m depth, + not fixed (Ref. 9.1.3, pg. 27) |

TABLE 6.10 – Fairness of Plating Between Frames

| Item | JSQS (Tolerance limits) | Rec. 47 (Limit) | VSM (Limit 95 / 5 %) |
| --- | --- | --- | --- |
| Shell plate | Parallel part (side & bottom shell) | 6 mm (Ref. IX.A.1, pg. 22) | 8 mm | 4 / 7 mm (Ref. 6.1.1, pg. 20) |
|  | Fore and aft part |  |  |  |
| Tank top plate |  | 7 mm (Ref. IX.A.2, pg. 22) |  | 6 / 8 mm (Ref. 6.1.1, pg. 20) |
| Bulkhead | Bulkhead Trans. Bulkhead Swash Bulkhead 4mm | 8 mm (Ref. IX.A.3, pg. 22) |  | 6 / 8 mm (Ref. 6.1.1, pg. 20) |
| Strength deck | Parallel part | 6 mm | 8 mm | ? |
|  | Fore and aft part Covered part | 9 mm 9 mm (Ref. IX.A.4, pg. 22) | 9 mm 9 mm | 4 / 6 mm 7 / 9 mm (Ref. 6.1.1, pg. 20) |
| Second deck | Bare part | 8 mm | 8 mm | 6 / 9 mm (Ref. 6.1.1, pg. 20) |
|  | Covered part | 9 mm (Ref. IX.A.5, pg. 22) | 9 mm |  |
| Forecastle deck Poop deck | Bare part | 6 mm | 8 mm | ? |
|  | Covered part | 9 mm (Ref. IX.A.6, pg. 22) | 9 mm | ? |
| Super structure Deck | Bare part | 6 mm | 6 mm | 4 / 6 mm |
|  | Covered part | 9 mm (Ref. IX.A.7, pg. 22) | 9 mm | 7 / 9 mm (Ref. 6.1.1, pg. 20) |
| House wall | Outside wall | 6 mm | 6 mm | 4 / 6 mm |
|  | Inside wall | 6 mm | 8 mm | 4 / 6 mm |
|  | Covered part | 9 mm (Ref. IX.A.9, pg. 22) | 9 mm | 6 / 8 mm (Ref. 6.1.1, pg. 20) |
| Interior member (web of girder, etc) | 7 mm (Ref. IX.A.10, pg. 22) | 7 mm | ? |
| Floor and girder in double bottom | 8 mm (Ref. IX.A.11, pg. 22) | 7 mm | ? |

TABLE 6.11 – Fairness of Plating with Frames

| Item | JSQS (Tolerance limits) | Rec. 47 (Limit) | VSM (Limit) |
| --- | --- | --- | --- |
| Shell plate | Parallel part | ± 3/1000 mm | ± 3 /1000 mm | ? |
|  | Fore and aft part | ± 2/1000 mm (Ref. IX.B.1, pg. 23) | ± 4 /1000 mm | ? |
| Strength deck (excluding cross deck) and top plate of double bottom | - | ± 4/1000 mm (Ref. IX.B.2, pg. 23) | ± 4 /1000 mm | ? |
| Bulkhead | - | ± 5/1000 mm (Ref. IX.B.3, pg. 23) | ± 5 /1000 mm | ? |
| Others | - | ± 6/1000 mm (Ref. IX.B.5, pg. 23) | ± 6 /1000 mm | ? |

TABLE 6.12 – Preheating for welding hull steels at low temperature

| Item | JSQS (Tolerance limits) | Rec. 47 (Limit) | VSM (Limit) |
| --- | --- | --- | --- |
|  | Base metal temperature needed preheating | Minimum preheating temperature |  |  |
| Normal strength steels | A, B, D, E | Below 0oC | 20oC 1) |  |  |
| Higher strength steels (TPMC type) | AH32 – EH 32 AH36 – EH 36 |  |  |  |  |
| Higher strength steels (Conventional type) |  |  |  |  |  |
| (Note) 1) This level of preheat is to be applied unless the approved welding procedure specifies a higher level. |

TABLE 7.1 – Alignment

| Detail | JSQS (Tolerance limits) | Rec. 47 (Limit) | VSM (Limit) |
| --- | --- | --- | --- |
| Alignment of butt welds | Strength member: a ≤ 0.15 t max. 3 mm Other: a ≤ 0.2 t max. 3 mm (Ref. VIII.C.4, pg. 19) | Strength member: a ≤ 0.15 t Other: a ≤ 0.2 t a ≤ 3.0 mm | Low: a ≤ 0.25 t max. 5 mm Medium: a ≤ 0.15 t max. 4 mm High: a ≤ 0.1 t max. 3 mm (Table 1, No. 18) |
| Alignment of fillet welds t1 < t2 | Strength member: a ≤ 0.333 t Other: a ≤ 0.5 t (Ref. VIII.C.3, pg. 17) | a) Strength and higher tensile: a ≤ t1/4 measured on the median. a ≤ (5t1- 3t2)/6 measured on the heel line. b) Other: a ≤ t1/2 measured on the median. a ≤ (2t1- t2)/2 measured on the heel line. | a ≤ 0.5 t (Ref. 5.4.1, pg. 17) |
| Alignment of fillet welds | ? | a) Strength and higher tensile: a ≤ t1/3 measured on the median a1 ≤ (5t1- 3t2)/6 measured on the heel line. b) Other: a1 ≤ t1/2 measured on the median a1 ≤ (2t1- t2)/2 measured on the heel line. | a ≤ 0.5 t (Ref. 5.4.2, pg. 18) |

TABLE 7.2 – Alignment

| Detail | JSQS (Tolerance limits) | Rec. 47 (Limit) | VSM (Limit) |
| --- | --- | --- | --- |
| Alignment of flange of T-longitudinal | ? | a = 8.0 mm | ? |
| Alignment of height of T-bar, L-angle bar or bulb | ? | 3.0 mm | ? |
| Alignment of panel stiffener | ? | ? | ? |
| Gap between bracket/intercostal and Stiffener | ? | 3 mm | ? |
| Alignment of lap welds | a ≤ 3 mm (Ref. VIII.C.3, pg. 19) | ? | ? |

TABLE 7.3 – Alignment

| Detail | JSQS (Tolerance limits) | Rec. 47 (Standard) | VSM (Limit) |
| --- | --- | --- | --- |
| Gap between beam and frame | a ≤ 5.0 mm (Ref. VIII.C.3, pg. 17) | a ≤ 2.0 mm | ? |
| Position of scallop | ? | d ≥ 75 mm | ? |
| Gap around stiffener cut-out | s ≤ 3.0 mm (Ref. VIII.B.2, pg. 16) | s ≤ 2.0 mm | ? |

TABLE 8.1 –Typical Butt Weld Plate Edge Preparation (Manual Welding)

| Detail | JSQS (Tolerance limits) | Rec. 47 (Limit) | VSM (Limit) |
| --- | --- | --- | --- |
| Square butt |  | t ≤ 5 mm G = 3 mm |  |
| Single level butt |  | t > 5 mm G ≤ 3 mm R ≤ 3 mm θ = 50° - 70° |  |
| Double bevel butt |  | t > 19 mm G ≤ 3 mm R ≤ 3 mm θ = 50° - 70° |  |
| Double vee butt, uniform bevels |  | G ≤ 3 mm R ≤ 3 mm θ = 50° - 70° |  |
| Double vee butt, non-uniform bevel |  | G ≤ 3 mm R ≤ 3 mm 6 ≤ h ≤ t/3 mm θ = 50° α = 90° |  |
| NOTE 1 Different plate edge preparation may be accepted or approved by the Classification Society on the basis of an appropriate welding procedure specification. For welding procedures other than manual welding, see paragraph 3.2 Qualification of weld procedures. |

TABLE 8.2 – Typical Butt Weld Plate Edge Preparation (Manual Welding)

| Detail | JSQS (Tolerance limits) | Rec. 47 (Limit) | VSM (Limit) |
| --- | --- | --- | --- |
| Single vee butt, one side welding with backing strip (temporary or permanent) |  | G = 3 - 9 mm θ = 30° - 45° |  |
| Single vee butt |  | G ≤ 3 mm θ = 30° - 70° R ≤ 3 mm |  |
| NOTE 1 Different plate edge preparation may be accepted or approved by the Classification Society on the basis of an appropriate welding procedure specification. For welding procedures other than manual welding, see paragraph 3.2 Qualification of welding procedures. |

Table 8.3 -Typical Fillet Weld Plate Edge Preparation (Manual Welding)

| Detail | JSQS (Tolerance limits) | Rec. 47 (Standard) | VSM (Limit) |
| --- | --- | --- | --- |
| Tee Fillet |  | G ≤ 2 mm | Low: max. 4 mm Medium: max. 3mm High: max. 2mm (Ref. Table 1, No. 10) |
| Small angle fillet |  | α = 50° -70° β = 70° - 90° G ≤ 2 mm |  |
| Single bevel tee with permanent backing |  | G ≤ 4 - 6 mm θ° = 30° - 45° |  |
| Single bevel tee |  | G ≤ 3 mm R ≤ 3 mm θ° = 50° |  |
| NOTE 1 Different plate edge preparation may be accepted or approved by the Classification Society on the basis of an appropriate welding procedure specification. For welding procedures other than manual welding, see paragraph 3.2 Qualification of welding procedures. |

Table 8.4 Typical Fillet Weld Plate Edge Preparation (Manual Welding)

| Detail | JSQS (Tolerance limits) | Rec. 47 (Standard) | VSM (Limit) |
| --- | --- | --- | --- |
| Single ‘J’ tee |  | G =2.5 - 4 mm r = 12 - 15 mm R = 3 mm θ ≥ 35° |  |
| Double bevel tee symmetrical |  | t > 19 mm G ≤ 3 mm R ≤ 3 mm θ = 50° |  |
| Double bevel tee assymetrical |  | t > 19 mm G ≤ 3 mm R ≤ 3 mm |  |
| Double J bevel symmetrical |  | G =2.5- 4 mm r = 12 -15 mm R ≤ 3 mm θ ≥ 35° |  |
| NOTE 1 Different plate edge preparation may be accepted or approved by the Classification Society on the basis of an appropriate welding procedure specification. For welding procedures other than manual welding, see paragraph 3.2 Qualification of welding procedures. |

Table 8.5 Typical Butt And Fillet Weld Profile (Manual Welding)

| Detail | JSQS (Tolerance limits) | Rec. 47 (Limit) | VSM (Limit) |
| --- | --- | --- | --- |
| Butt weld toe angle (and weld overfill ??) | θ ≤ 90° h not defined (Ref. VII.A.1, pg. 14) | θ ≤ 60° max. h = 6 mm | Low: max. 10 mm Medium: max. 7mm High: max. 5mm (Ref. Table 1, No. 12) |
| Butt weld undercut | Skin plate and face plate midship, over 90 mm continuous: D = 0.5 mm Other: D = 0.8 mm (Ref. VII.A.2, pg. 14) | 0.5 mm | Low: max. 1,5 mm Medium: max. 1,0mm High: max. 0,5mm (Ref. Table 1, No. 11) |
| Fillet weld leg length s = leg length a = throat depth | s ≥ 0.9sd a ≥ 0.9ad sd= design s ad= design a (Ref. VII.A.3, pg. 14) | s ≥ 0.9sd a ≥ 0.9ad over short weld lengths sd= design s ad= design a | a ≥ 0.9 ad – 0,3 mm Low: max. 2 mm Medium: max. 1mm High: Not permitted (Ref. Table 1, No. 15) |
| Fillet weld toe angle | θ ≤ 90° (Ref. VII.A.3, pg. 14) | θ ≤ 90° In areas of stress concentration and fatigue, the Class Society may require a lesser angle. | ? |
| Fillet weld undercut | D = 0.8 mm (Ref. VII.A.2, pg. 14) | D = 0.5 mm | Low: D = 1,5 mm Medium: D = 1,0 mm High: D = 0,5 mm (Ref. Table 1, No. 11) |

Table 8.6 Typical Lap, Plug and Slot Welding (Manual Welding)

| Detail | JSQS (Tolerance limits) | Rec. 47 (Standard) | VSM (Limit) |
| --- | --- | --- | --- |
| Fillet weld in lap joint | ? | b = 2t2 + 25mm location of lap joint to be approved by the Classification Society |  |
| Fillet weld in joggled lap joint | ? | b ≥ 2 t2 + 25 mm |  |
| Plug welding | ? | when t ≤12 mm l = 60 mm R = 6 mm, 40°-50° G = 12 mm L > 2l when 12< t ≤ 25 mm l = 80 mm R = 0.5t mm, 30° G = t mm L > 2l |  |
| Slot welding | ? | when t ≤12 mm l = 80 mm G = 20 mm L= 2l-3l max. 250mm when t > 12 mm l = 100 mm G = 2t L = 2l-3l max. 250 mm |  |

Table 8.7  Distance Between Welds Table

| Detail | JSQS (Tolerance limits) | Rec. 47 (Standard) | VSM (Limit) |
| --- | --- | --- | --- |
| Scallops over weld seams | for main structure d ≥ 5 mm for other structure d ≥ 0 mm (Ref. VIII.A.2, pg. 16) | for r ≥ 30 mm d ≥ 5 mm The “d” is to be measured from the toe of the fillet weld to the toe of the butt weld. | d ≥ 10 mm (Ref. 5.5.2, pg. 19) |
| Distance between two butt welds | d ≥ 0 mm (Ref. VIII.A.1, pg. 16) | d ≥ 0 mm | d optional, if measures have been taken for a satisfactory welding of butt welds (Ref. 5.2.1, pg. 19) |
| Distance between butt weld and fillet weld | for main structure d ≥ 10 mm for other structure d ≥ 0 mm (Ref. VIII.A.2, pg. 16) | d ≥ 10 mm | Fillet weld first: d ≥ 30 mm + 2 t Butt weld first: d ≥ 10 mm (Ref. 5.5.1, pg. 19) |
| Distance between butt welds | for cut-outs d ≥ 30 mm (Ref. VIII.A.1, pg. 16) | for cut-outs d ≥ 30 mm | for cut-outs d ≥ 50 mm + 4 t (Ref. 5.5.1, pg. 19) |
|  | ? | for margin plates d ≥ 300 mm limit: 150 mm (??) | ? |

8.8 - Automatic Welding Table

| Detail | JSQS (Tolerance limits) | Rec. 47 (Limit) | VSM (Limit) |
| --- | --- | --- | --- |
| Submerged Arc Welding (SAW) | One side SAW: G ≤ 5 mm (Ref. VIII.C.2, pg. 18) Both side SAW: G ≤ 2 mm (Ref. VIII.B.1, pg. 18) | G ≤ 5 mm Edge preparation as per Tables 8.1 and 8.2 SAW may follow WPS approved by the Classification Society. See Note 1. | According to welding procedure; if G is larger than specified, then gaps up to G = t, max. 300 mm may be closed build-up welding trimmed to the required gap width (Ref. 5.2.3, pg. 17) |
| NOTE 1 Different plate edge preparation may be accepted or approved by the Classification Society on the basis of an appropriate welding procedure specification. For welding procedures other than manual welding, see paragraph 3.2 Qualification of welding procedures. |